| RETRACTABLEAWNINGS.COM WIND RAIN BUG ZIP® PERFORMANCE DATA |
| --- |
|  | Result: Permissible Tension Tmax Tmax=Fmax / W=13.5�E�Eg/cm EE/td> Conditions: ·2SL-FCOAT PT16 Series Slide-Fastener. ·33mm Guide-Rail System. ·NH6 PVC Inner-Rail Rain Flow Rate: 4l/m² per minute; Permissible Pressure: 250Pa∼750Pa(5.5kg/m²∼76.5kg/m²) Permissible Wind Pressure: ±3,600Pa(±367kg/m²) Test Fabrics: Mesh type fiberglass: SERGE(eqv.21136#) Test: Weight-ball(1Kg) drops from different heights toward the screen. Result: Center Fabrics is broken first before the Slide-Fastener structure. Test Fabrics: Mesh type fiberglass: SERGE(eqv.21136#) In general, all common-used fabrics can be applied for ordinary size window screen except very thin polyester fabrics. Recommendation ·PVC Coating Fiber glass (better welding performance and less stretching rate); Thicker fabrics are good for rolling performance. |